Name___________________                   			 Date_____________________

ENGAGE: Making Metals

- Three properties of metals:

3.

- An ________ is a mixture of two or more elements that is made up of at least one metal. Examples include: brass, bronze, steel.

EXPLORE:

One method of moving heat called __________ is when thermal energy travels through a solid. Metals are generally good conductors.  However, heat conductivity is a physical property that varies from metal to metal.  Although metals are generally good conductors, not all metals conduct heat equally. This activity involves rods of five different materials:

- Aluminum (Al) a pure metal

- Copper (Cu) a pure metal

- Nickel (Ni) a pure metal

- Brass, an alloy made of Copper (Cu) and Zinc (Zn)

- Stainless steel, an alloy made of Iron (Fe), Carbon (C), and Chromium (Cr)

Problem: Which type of metal is the best conductor of heat?

Hypothesis: If brass, stainless steel, aluminum, copper, and nickel are exposed to heat through a lit candle, then ____________will melt the wax at the end of the metal rod first.

Materials:

- Conductometer Rod (Conduction Wheel)

- Tea-light candle

- Wax

- Timer

Safety Precautions:

- Heating metals- wear goggles                           insert wax here

- Hot Liquids- Goggles/gloves

Procedure:

  - Insert wax in each indentation at the end of each spoke on the conductometer.

  - Light candle or burner. Place the conductometer above the flame BUT NOT TOUCHING IT! You want it to be about an inch or so above the flame.

  - Begin timing your trials now. You want to observe the wax as the rod is heated- record when it melts on each metal rod.

Data Collection:

| Name of Metal or Alloy | Time to Melt Wax Group 1 | Time to Melt Wax Group 2 | Time to Melt Wax Group 3 | Time to Melt Wax Group 4 | Time to Melt Wax Group 5 | Time to Melt Wax Group 6 |
| --- | --- | --- | --- | --- | --- | --- |
| Aluminum |  |  |  |  |  |  |
| Copper |  |  |  |  |  |  |
| Nickel |  |  |  |  |  |  |
| Brass |  |  |  |  |  |  |
| Stainless Steel |  |  |  |  |  |  |

EXPLAIN

- Sequence your results from the least amount of time for the wax to melt to the most amount of time for the wax to melt.

____________________________________________________________________________________________________________________________________________________________________________________________________________________________________

- What is the independent variable in this experiment?_________________________

- What is the dependent variable in this experiment?__________________________

- What other variables account for the fact that not all groups recorded the exact same times for each material to melt the wax?__________________________________________________

- Did the data support my hypothesis? Why or why not?_________________________________

_________________________________________________________________________

ELABORATE: METALS AND ALLOYS AROUND THE HOUSE

Copper	 						steel

- ___________________ is used as a frame for houses and buildings. Why is this a good choice?_____________________________________________________________

- ___________________ is used as a heating element to cook on. Why is this a good choice? ____________________________________________________________________

- Name two other alloys and metals you can find in your house and describe what they are used for.__________________ is used to ______________________________________

_______________ is used to ___________________________________________